# MODELLING OF PHENOLIC RESIN POLYMERISATION

## C.C.RICCARDI a,*, G. ASTARLOA AIERBE b, J.M. ECHEVERRÍA c and I.MONDRAGÓN b

a Institute of Materials Science and Technology (INTEMA) University of Mar del Plata and National Research Council (CONICET) Av. J. B. Justo 4302,  7600 Mar del Plata, Argentina

b Dpto. Ingeniería Química y Medio Ambiente. Escuela Ingeniería Técnica Industrial. Universidad del País Vasco/ Euskal Herriko Unibertsitatea. Av. Felipe IV  1-B,  20011 San Sebastián/Donostia , Spain

c Bakelite-Ibérica, Ctra. A Navarra, Epele, 39, 20120 Hernani, Spain

* To whom correspondence should be addressed

(

ABSTRACT

Key words: Modellisation- Resol- Phenolic Resin-Kinetic-Mechanism

### INTRODUCTION

EXPERIMENTAL

##### Synthesis of resols

Fourteen prepolymers were synthesized by varying the type or amount of catalyst, the initial formaldehyde to phenol (F/P) molar ratio, the condensation temperature, or the initial pH. Table 1 shows the name, formulation and synthesized conditions for each resol.

Phenol (>99%), formaldehyde (37% aqueous solution) and alkaline catalyst were commercial products used without further purification.

Prepolymers were prepared in the IQU-Bakelite factory by mixing phenol and formaldehyde aqueous solution, with the desired molar ratio, in a three necked flask equipped with a thermometer, stirred, and refrigeration column. The pH was then adjusted with the necessary amount of the corresponding alkaline catalyst. The mixture was heated to the selected condensation temperature (heating rate: 2.5-3.5ºC/min) and stirred during reaction. Samples were taken during synthesis. Zero time was defined as time to the mixtures reached the condensation temperature. The reaction was stopped putting the reactor in a cold-water bath, when the resin showed a 1/1 g/g dilutability in water. Samples were kept at 4ªC.

High performance liquid chromatography (HPLC)

Analyses were conducted with a Waters 510 chromatograph equipped with a Waters 486 u.v. detector, set at 280nm. The columns were Spherisorb ODS-2  (5(m). In order to decrease the viscosity of the solvents, the columns were thermostatted to 35ºC. A mobile phase of methanol/water was used with an elution gradient of 20% to 80% of methanol in 180 min, and 80% to 100% in 5 min.

Experimental results

The evolution of free formaldehyde during synthesis was followed by chemical assay8, while the disappearance of phenol and formation of addition and condensation products were quantitatively followed by liquid cromatography

##### MODEL FORMULATION

RESULTS AND DISCUSSION

CONCLUSIONS

AKNOWLEDGEMENTS

REFERENCES

#### TABLES

Table 1:  Formulations and synthesized conditions for each prepolymer

| Name | Catalyst | Temperature (ºC) | F/P | Amount of catalyst (g/500g of phenol) | pH | Initial phenol concentration (mol/L) |
| --- | --- | --- | --- | --- | --- | --- |
| RNa | Na(OH) | 80 | 1.8 | 5.7 | 8 | 4.36 |
| RZn | Zn(CH3COO)2(H2O | 80 | 1.8 | 11.7 | 8 | 4.34 |
| RBa | Ba(OH)2 | 80 | 1.8 | 3.75 | 8 | 4.36 |
| RT60 | (CH3CH2)3N | 60 | 1.8 | 8.6 | 8 | 4.35 |
| RT95 | (CH3CH2)3N | 95 | 1.8 | 5.7 | 8 | 4.36 |
| RT43 | (CH3CH2)3N | 80 | 1.8 | 4.3 | 8 | 4.36 |
| RT84 | (CH3CH2)3N | 80 | 1.8 | 8.4 | 8 | 4.35 |
| RT199 | (CH3CH2)3N | 80 | 1.8 | 19.9 | 8 | 4.31 |
| RT10 | (CH3CH2)3N | 80 | 1.0 | 13.0 | 8 | 5.91 |
| RT14 | (CH3CH2)3N | 80 | 1.4 | 8.5 | 8 | 5.02 |
| RT22 | (CH3CH2)3N | 80 | 2.2 | 7.8 | 8 | 3.83 |
| RT26 | (CH3CH2)3N | 80 | 2.6 | 5.4 | 8 | 3.43 |
| RT823 | (CH3CH2)3N | 80 | 1.8 | 20.0 | 8.23 | 4.31 |
| RT836 | (CH3CH2)3N | 80 | 1.8 | 20.0 | 8.36 | 4.31 |

#### FIGURE LEGENDS

# Footnotes

( E-mail: criccard@fi.mdp.edu.ar  - TEL:  54 0223 481 6600 – FAX: 54 0223 481 0046